## Slide 1
Fiber to chip packaging with low loss for quantum applications
Juniyali Nauriyal, Meiting Song, Marissa Granados-Baez, Yi Zhang , Jaime Cardenas
REFERENCES
Order online at https://www.postersession.com/order/
Acknowledgement
We would like to thank Hajim School of Engineering and Applied Sciences, AIM Photonics and Cornell NanoScale Science & Technology Facility
Barwicz, Tymon, et al. "A Novel Approach to Photonic Packaging Leveraging Existing High-Throughput Microelectronic Facilities." IEEE Journal of Selected Topics in Quantum Electronics 22.6 (2016): 455-466.
Shimizu, N. (Mar. 1984). Fusion splicing between deposited silica waveguides and optical fibers. Electronics and Communications in Japan (Part I: Communications), 67(9), 115-122. doi:10.1002/ecja.4400670914;
J. Nauriyal, M. Song, R. Yu, and J. Cardenas, “Fiber-to-chip fusion splicing for low-loss photonic packaging,” Optica, OPTICA, vol. 6, no. 5, pp. 549–552, May 2019, doi: 10.1364/OPTICA.6.000549
ABSTRACT
One of the remaining challenges to achieve manufacturing scalability of silicon nanophotonic devices is a low cost, highly efficient, and mechanically robust method to optically couple multiple optical fibers to a photonic chip at once. We present a robust, low-loss packaging technique of permanent optical edge coupling for quantum applications between a single/multiple fibers and a chip using fusion splicing that is low-cost and scalable for high-volume manufacturing. We fuse the fiber array to the chip via a CO2 laser and reinforce it with an optical adhesive. We demonstrate a minimum loss of 1.0 dB per facet with 0.6 dB penalty over a 160 nm bandwidth from 1480 to 1640 nm for single fiber. We measure a minimum loss of 2.5dB per facet with a variation of +/-0.1dB across a 4-fiber array. We also compared losses with a 2 fiber and a single fiber which is 2.2dB and 1.0dB respectively.
BACKGROUND
Silicon photonics faces a major challenge in terms of manufacturing scalability due to its high packaging cost, tight alignment tolerance of the fiber to chip and coupling inefficiency[1,2].
80-90% of the cost of the photonic device comes from packaging and testing.
We fusion splice a fiber to a chip using a CO2 laser with low loss, low cost and large misalignment tolerance of +/-2.5um.
APPROACH
Optical Fiber
MFD= 10.4um
CO2 Laser fusing
Photonic chip
Waveguide Taper
Oxide Mode
Converter
Fusion Spot
Laser light
at 30֯
Fig 1) Fiber attach process for a single fiber (MFD 10.4um) to a photonic chip with an oxide mode converter. The red spot shows the splicing area between the optical fiber and the photonic chip.
The single fiber attach technology[3] shown in figure 1 is then applied to a fiber array of 2 and 4 fibers with the mode field diameter(MFD) of 10.4um.
The fusion is done using an elliptical beam of the CO2 laser which helps in splicing the fiber array to the chip in a single shot, see figure 2.
The multiple splicing technology does not require any additional ferrules or adhesives to package the device and the fiber.
Nitride
tapers
4-fiber array
TOP VIEW
Mode converter
Photonic chip
Fusion Spot from laser
250µm
U-grooves
125µm
Single fiber splicing
Fiber array splicing
Fig 2) Schematic representation of the top view of the method shows the fusion splicing spot from the CO2 laser and the u-grooves for aligning fiber arrays to the photonic chip.
The fiber arrays have a pitch of 125um and MFD of 10.4um. The laser beam is elliptical to fuse multiple fibers in a single shot.
METHODS
Device fabrication and fusion process
Nitride
taper
SiO2Mode
Converter
TOP VIEW
Undercut silicon
substrate
14μm
12μm
Fiber array
Photonic
chip
Fig 3) Microscope image of the fabricated device, with oxide mode converter, silicon nitride waveguide taper and undercut silicon substrate(left). Photograph of a packaged photonic device with 3 fibers fused to the photonic chip using fusion splicing(right). The packaged device does not require adhesive or ferrules for support and stability.
As the beam is focused into a line, it is aligned at the fiber to mode converter interface for an exposure of 1 sec at 10W +/-2W of laser power. The width (3mm) is selected to enable fusing a 12-fiber array in a single shot for future applications.
RESULTS
Fig 4) Coupling loss of single fiber, 2 fiber and 4 fiber array was measured as 1.2dB, 2.2dB and 2.5dB per-facet respectively.
We fuse a cleaved 1,2 and 4-fiber array to the oxide mode converter using a single shot from the CO2 laser and measure a coupling loss of 1.2dB, 2.2dB and 2.5dB per-facet respectively. A waveguide propagation loss of 0.4dB was subtracted from the measured loss. We expect to see a decrease in the coupling loss after the application of an optical adhesive is applied after the fusion to optimize mode matching [3]. We measure variation of +/- 0.1dB across a 4 fiber-array at 1550nm and +/-0.05dB across a 2-fiber array at 1550nm as shown in figure 4.