## Slide 1: Fibre-optic Quantum Entanglement Sources
July 24, 2020
Li Qian
Department of Electrical & Computer Engineering, University of Toronto

## Slide 2: Acknowledgement
Graduate students and postdocs
  Arash Riazi
  Changjia Chen
  Dr. Eric Zhu
Colleagues
  Prof. John Sipe – (Toronto)
  Prof. Peter Kazansky (Southampton)
  Dr. Alexey Gladyshev (Russia)
Postdoc Position Open: l.qian@utoronto.ca

## Slide 3: Photon sources as an enabler
Market
Optical
Technology
First entangled source
Quantum
Technology
1960
1970
1980
1990
2000
2010
2020
2030
Year
First laser
$650B
More practical, more variety
More practical more variety
Notes: Photonics industry source: PHOTONICS MARKET - GROWTH, TRENDS, AND FORECAST (2019 - 2024), Mordor intelligence, https://www.mordorintelligence.com/industry-reports/photonics-market-market

## Slide 4
A Practical Source
A Versatile Source

## Slide 5: Broadband Polarization Entangled Source
E Y. Zhu, L. Qian et al., PRL, 108, 213902, 2012
E Y. Zhu, L. Qian et al., Opt. Lett., 38, 4397, 2013
C. Chen, L. Qian et al., Opt. Express, 25, 22668, 2017
C. Chen, L. Qian et al., OSA Continuum, 1, 981, 2018
Room-temp, Alignment-free, Compensation-free
Periodically-Poled Silica Fiber
c(2) SPDC in PPSF
https://www.ozoptics.com/ALLNEW_PDF/DTS0158.pdf

## Slide 6: The making of PPSF
(2)= 0
y
x
Efficient 3-wave mixing
periodic UV erasure
Thermal Poling
y
x
P.G. Kazansky and P.St.J. Russell, Optics Comm. 110, 611 (1994).
Margulis et al., Opt. Express 17, 15534 (2009)
J. Zhang and L. Qian, JOSA B, 26, 1412 (2008)
P. G. Kazansky et al., Opt. Lett. 34, 2483 (2009)
E. Y. Zhu et al., Opt. Lett. 35, 1530 (2010), JOSA B 27, 2410 (2010)
H. An and S. Fleming, Opt. Express, 20, 7436 (2012)

## Slide 7: Birefringent phase matching
768 769 770 771 772 773 774 775 776
SHG Conversion Efficiency ( 10-4 W -1)
Type II
Notes: Multiple sets of frequencies that satisfy phase matching condition

## Slide 8: Type II SPDC spectrum
768 769 770 771 772 773 774 775 776
SHG Conversion Efficiency ( 10-4 W -1)
Pump wavelength (nm)
Signal/Idler wavelength (nm)
Type II SPDC Tuning Curve
pump
Type II
1490
1550
1610
1490
1550
1610
signal (nm)
idler  (nm)
Biphoton Spectral Intensity

## Slide 9: Temporal and spectral distinguishabilities
lidler
lsignal
V-polarized
H-polarized
lidler
lsignal
H-polarized
V-polarized
|f|2
|g|2
Temporal distinguishability
Spectral distinguishability

## Slide 10: Compensation-free condition
Compensation-free hyper-entangled source is possible!
Both spectral & temporal distinguishabilities are negligible
C. Chen, L. Qian et al., Opt. Express, 25, 22668, 2017
Chromatic Dispersion >> Polarization Mode Dispersion

## Slide 11: Concurrence and bandwidth
Without
compensation
C. Chen, L. Qian et al., Opt. Express, 25, 22668, 2017
80nm

## Slide 12: Performance
https://www.ozoptics.com/ALLNEW_PDF/DTS0158.pdf

## Slide 13
A Practical Source
A Versatile Source

## Slide 14: Variety, variety, variety
Variety of Lasers | Time Domain | Frequency Domain | Polarization
 | Continuous-wave | Narrow linewidth | Linear. Circular, Elliptical, Depolarized
 | Mode-locked pulse train | Broadband frequency combs | 
 | Arbitrary waveform | Arbitrary spectral shaping | 
Variety of | Single photons | Time Domain | Frequency Domain | Polarization
 |  | Continuous-wave, Pulsed | Narrow linewidth Broadband | Linear, Circ., Ellipt.

## Slide 15: Variety, variety, variety
Variety of Lasers | Time Domain | Frequency Domain | Polarization
 | Continuous-wave | Narrow linewidth | Linear. Circular, Elliptical, Depolarized
 | Mode-locked pulse train | Broadband frequency combs | 
 | Arbitrary waveform | Arbitrary spectral shaping | 
Variety of | Single photons | Time Domain | Frequency Domain | Polarization
 |  | Continuous-wave, Pulsed | Narrow linewidth Broadband | Linear, Circ., Ellipt.
 | Bi-photons | Long vs short correlation time Periodically recurrent correlations Arbitrarily shaped temporal correlation | Spectrally correlated vs. uncorrelated Biphoton frequency combs Arbitrary shaped spectral correlation | Entangled Partially entangled Arbitrary state
There is a much larger “space” to explore for biphoton sources

## Slide 16: Existing methods of biphoton spectral shaping
Problems:
Wasteful due to filtering
High loss due to coupling
Problems:
Not easily tunable – fixed spectral shape
Fabrication technology dependent
Neither system is capable of shaping polarization at the same time
biphoton generation in simple nonlinear medium
External Spectral
shaping
biphoton generation in complex nonlinear medium
Weiner et al. OL, 43, 743, 2018
e.g.
e.g.
Sergienko et al. OE, 24, 24947, 2016

## Slide 17: biphoton shaping – nonlinear interference
biphoton generation in simple nonlinear medium (DkL)

## Slide 18: Simultaneous spectral and polarization shaping
}
biphoton generation in simple nonlinear medium (DkL)
biphoton generation in simple nonlinear medium (DkL)
Dispersion
Polarization
Rotation
Linear medium
Spectral
shaping
Polarization
shaping
Riazi, L. Qian et al., npj Quantum Information, 5, 77, 2019
A. Riazi, L. Qian et al., CLEO 2020, FM2C.7

## Slide 19: All-fiber implementation - reflection
Common-path configuration: pump, signal, idler travel in the same mode and same path – complete phase stability
PPSF
PC
Broadband reflector
+ inline polarization controller
broadband
reflector
Nonlinear section:
PPSF
Linear Section:
Dispersive fiber
WDM

## Slide 20: Results: 2-element interference

## Slide 21: Results: 2-element cascade
Emission Spectrum a.u.
Wavelength(nm)
Experiment

## Slide 22: “Arbitrary” spectral shaping
Multiple-element (N≤5) cascade with various linear elements in between

## Slide 23: Polarization shaping – incoherent cascade

## Slide 24: Polarization shaping – incoherent cascade
Output States | Fidelity to | Concur-rence
PPSF 1 |  | 
PPSF 2 |  | 
Output States |  | Concur-rence
PPSF 1 |  | 
PPSF 2 |  | 
Table 1. Fidelity and concurrence of the biphoton state measured in polarization basis.
A. Riazi, L. Qian et al., npj Quantum Information, 5, 77, 2019
Notes: Incoherent cascade

## Slide 25: Spectral and polarization DoF coupling
}
biphoton generation in simple nonlinear medium (DkL)
biphoton generation in simple nonlinear medium (DkL)
Dispersion
Polarization
Rotation
Linear medium
Spectral
Polarization
Riazi, L. Qian et al., npj Quantum Information, 5, 77, 2019
A. Riazi, L. Qian et al., CLEO 2020, FM2C.7

## Slide 26: l-dependent concurrence
PPSF
Linear dispersive fiber
broadband
reflector
+ inline polarization controller
WDM
A. Riazi, L. Qian et al., CLEO 2020, FM2C.7
Notes: Coherent cascade

## Slide 27: Wavelength-dependent polarization entanglement
PPSF
Linear dispersive fiber
+ inline polarization controller
broadband
reflector
Trace over Polarization DoF
WDM
A. Riazi, L. Qian et al., CLEO 2020, FM2C.7
Notes: Coherent cascade

## Slide 28: Fibre-based common-path NLI
Novel strategy for biphoton shaping:
  cascading and interfering biphotons from multiple nonlinear sources
  Particularly suited for PPSF-based broadband polarization-entangled sources
Major advantages:
  Simultaneous shaping of spectrum and polarization
  Can be used to generate arbitrary biphoton polarization states
  Tuning the degree of polarization entanglement through frequency tuning
  Common-path configuration: guaranteed phase stability
  Low loss and efficient: all-fiber construction; no post-selection or filtering
Significance:
  A practical way to create versatile entangled biphoton sources

## Slide 29: Current and Future Directions
Versatile and tunable entangled photon sources
  Fibre-based broadband entanglement source
  Tunable spectral shape
  Tunable polarization states
  Tunable temporal shape
  Spatially separate hyper-entangled source (polarization + frequency bin)
Applications for entangled photon sources
  Entanglement-based Quantum Key Distribution
  Entanglement distribution in networks
  Clock synchronization
  Quantum measurements
  Quantum sensing

## Slide 30: Entanglement based QKD
EY Zhu, L. Qian et al., JOSA B, 36, B1-6, 2019

## Slide 31: Dispersion measurement using biphotons
A Riazi, L. Qian et al., Opt. Lett., 44, 1484, 2019
A Riazi, L. Qian et al., Opt. Lett., 45, 2034, 2020
Nonlinear section:
PPSF
Linear Section:
Dispersive fiber
WDM

## Slide 32: Summary
Periodically-Poled Silica Fiber
c(2) SPDC in PPSF
Nonlinear section
Linear Section
WDM
PPSF
Pol Ctrl + Dispersion
Applications:
Arbitrary biphoton state generation
Quantum network – entanglement distr.
Metrology – dispersion, phase measurements

## Slide 33: Acknowledgement
Graduate students and postdocs
  Arash Riazi
  Changjia Chen
  Dr. Eric Zhu
Colleagues
  Prof. John Sipe – (Toronto)
  Prof. Peter Kazansky (Southampton)
  Dr. Alexey Gladyshev (Russia)
Postdoc Position Open: l.qian@utoronto.ca