## Slide 1: Backside illuminated CMOS active pixel sensor with global shutter and 84 dB dynamic range
G. Meynants, G. Beeckman, W. Ogiers, K. Van Wichelen, J. Bogaerts
CMOSIS NV, Antwerp, Belgium
Scientific Detector Workshop – Firenze – 8 October 2013

## Slide 2: The problem(s) (where we started with)
Backside Illuminated Thinned Focal Plane Array “BITFPA”
Characteristic:
Large dynamic range: 84 dB
FWC > 400,000 e- & Noise < 25 e- RMS
Global shutter
Backside illuminated
QE: 50% 270-400 nm
75% QE 400-800 nm
1k x 1k pixels, 16 Hz
10-20 µm pixel size

## Slide 3: Outline
Pixel architecture
  Dynamic range
  BSI compatible global shutter
Architecture
Backside thinning
  Process flow
  Hot pixel cluster issues
Work in progress

## Slide 4: Dual gain channel global shutter pixel Pixel schematic

## Slide 5: Dual gain channel global shutter pixel Pixel schematic
Photodiode & charge sense amplifier
Sample reset & signal
high gain
Sample reset & signal
low gain

## Slide 6: Dual gain channel global shutter pixel Pixel timing
high gain signal
high gain reset
low gain reset
low gain signal
Timing at end of exposure
Synchronous in all pixels

## Slide 7: Timing – 1. End of exposure, after FD reset

## Slide 8: Timing – 2. First charge transfer

## Slide 9: Timing – 3. Sampling of high gain signal

## Slide 10: Timing – 4. activate HDR switch

## Slide 11: Timing – 5. 2nd charge transfer

## Slide 12: Timing – 6. sample low gain signal

## Slide 13: Pixel implementation and measured FSI characteristics
Pixel pitch | 20 x 20 µm2 | 
In-pixel capacitors | 2x MiM 150 fF 2x MOS 150 fF | 
Process | 0.18 µm 4LM CIS | 
Channel | High gain | Low gain
Conv. gain | 13 µV/e- | 1.5 µV/e-
FWC 2.8 V 3.3 V | 45 000 e- 58 000 e- | 450 000 e- 510 000 e-
Dark current @ RT, FSI | 6000 e-/s | 6000 e-/s
Noise | 20 e- RMS | 150 e- RMS
FSI characterisation on testchip and FSI prototypes

## Slide 14: Image sensor architecture

## Slide 15: Readout chain & noise budget
 |  |  | LOW-GAIN | HIGH-GAIN
Pixel |  |  |  | 
 | Conversion Gain @ pixel output | [V/e-] | 1.50E-06 | 13.00E-06
 | Swing at pixel output | [V] | 0.77 | 0.75
 | FWC | [e-] | 513.33E+03 | 57.69E+03
 | Noise @ pixel output | [Vrms] | 268.00E-06 | 268.00E-06
 | input referred noise | [e-rms] | 178.7 | 20.6
Column Gain Stage + S/H |  |  |  | 
 | Max. input swing (column) | [V] | 1.80 | 1.80
 | Column swing | [V] | 0.77 | 0.75
 | capacitor ratio CFF/CFB |  | 2.40 | 2.40
 | amplifier Acl |  | 2.38E+0 | 2.38E+0
 | Noise Generated | [Vrms] | 302.85E-06 | 302.85E-06
 | Max. output swing | [V] | 1.90 | 1.90
Signal Properties On S/H Caps |  |  |  | 
 | Sampled Signal Noise | [Vrms] | 706.04E-06 | 706.04E-06
Column Multiplexer |  |  |  | 
 | Noise Generated | [Vrms] | 304.06E-06 | 304.06E-06
Signal Properties On CDS Input |  |  |  | 
 | Signal Noise | [Vrms] | 763.62E-06 | 763.62E-06
 | Input Referred Noise | [e-rms] | 215.6 | 24.9
Output Stage (incl. CDS) |  |  |  | 
 | simulated noise | [Vrms] | 313.00E-06 | 313.00E-06
Signal Properties After output stage |  |  |  | 
 | Signal Noise | [Vrms] | 825.28E-06 | 825.28E-06
 | Input Referred Noise | [e-rms] | 233.0 | 26.9
 | Signal Swing | [V] | 1.82 | 1.77
 | Input Referred Swing | [e-] | 513.33E+03 | 57.69E+03
 | Conversion Gain | [V/e-] | 3.54E-06 | 30.69E-06
Dynamic Range |  |  |  | 
 | channel | [dB] | 66.86 | 66.63
 | overall | [dB] | 85.62 | 
Noise (output) low gain: 233 e- RMS
high gain : 27 e- RMS

## Slide 16: Noise and SNR – dual gain

## Slide 17: SOI based thinning flow
1. SOI Start material – 3 to 10 µm
3. Bonding of handling wafer after CMOS processing
2. Standard CMOS processing (on SOI substrate)
Notes: ----- Notulen (10/06/13 22:56) -----
tekening updaten, verwijder backside passivation

## Slide 18: BSI thinning flow (2)
4. Remove substrate under BOX – accurate thinning
5. Remove BOX
6. BSI passivation + AR coating, pad opening

## Slide 19: Quantum efficiency: separate process optimization for UV/VIS
270-400 nm > 50%
Optimized thickness
  3 µm epi-layer on SOI
Optimized ARC
  Al2O3 layer – thinner layer
Backside passivation through Al2O3 layer: fixed negative charge in the Al2O3
400-800 nm > 75%
Optimized thickness:
  10 µm epi-layer on SOI
Optimized ARC
  Al2O3 layer – tuned thickness
Backside passivation through Al2O3 layer

## Slide 20: Sapphire (Al2O3) deposition
Fixed negative charge (9.6e-12/cm2 reported in solar cell research)
This can compensate for the valley in the the electric field caused by the outdiffusion of backside boron implantation.

## Slide 21: First images on first SOI prototypes: large hot clusters
BSI (other product)
10 µm pixel, gray image
3 µm epitaxial layer
FSI on SOI, BITFPA
20 µm global shutter pixel, dark
10 µm epitaxial layer
More and larger clusters with higher supply voltage and thicker epi layer and strong increase of I(array) on SOI vs. bulk

## Slide 22: 10 µm BSI EUV dual-gain-per-pixel imager
Low gain channel
High gain channel

## Slide 23: 10 µm BSI dual gain pixel temperature dependency
Low gain channel
High gain channel
Stronger at lower temperature

## Slide 24: EMMI – NIR channel
NIR light emission in hot clusters
Electroluminescence
 Hot cluster = self-absorption of emitted photons
More clusters and more emission at higher pixel supply levels
BITFPA FSI imager processed on SOI – 20 µm pixel

## Slide 25: Pixel detail – SF drain emission center
Pixel with a metal top plate (BSI design, 20 µm global shutter)
SF drain
Layout
EMMI microscope

## Slide 26: Pixel detail – RST drain emission center
RST drain

## Slide 27: Vertical gettering in bulk CMOS wafers
Notes: the gettering layer is an impurity trapping site
the layer is created by precipitation of supersaturated oxigen
this creates stress, leading to stacking faults and dislocation loops
this forms a trapping site for the impurity
When the impurity is located in the gettering layer, it has no influence
any more on the device at the top of the wafer (photodiodes or mosfets)
This is known as intrinsic gettering.
Alternative gettering techniques exist (extrinsic gettering)

## Slide 28: Lack of vertical gettering in SOI wafer

## Slide 29: Electroluminescence in Si?
In Si very low band-to-band radiative recombination rate (indirect bandgap material) – phonon-assisted transition needed
Impurity or crystal defect can replace the role of the phonon
  Sub-bandgap energy emission.
  Not what we see here, energy of detected luminescent photons > band gap
Hot carriers in strong electric fields
H. Ivey, Electroluminescence and Semiconductor Lasers IEEE J. Quantum electronics, Vol. QE-2, No.11, Nov 1966
Transitions involving impurities
Interband transitions
  Intrinsic emission
  Higher energy emission involving “hot” carriers (“avalanche emission”)
Interband transitions involving hot carriers (“deceleration emission”)
But where do these hot carriers come from? And why are there so many?

## Slide 30: And why emission at the HV n+ areas?
Gettering of defects in n+ area:
  Some impurities may bind to the Phosphor at the n+ area
  For example Fe may form Fe-P pair in n+, inside or outside the space charge region
  Fe-B may also be formed (in the p-well for example)
The defect decreases avalanche breakdown voltage of the junction.
Strong E-field over reverse biased p-well/n+ junction at N+ supply diffusions causing avalanche breakdown -> hot carriers -> photoemission

## Slide 31
We could make light emitting pixels for a monolithic display…
This was already proposed on 1965 ISSCC by R.H. Dyck of Fairchild Semiconductor

## Slide 32: Fix
Before
After
Dark image 50ºC, 500 ms
Demonstrated on 10 µm SOI FSI device

## Slide 33: Conclusion
Image sensor in development with 84 dB and a dual-gain global shutter pixel architecture
  High gain channel with low noise
  Low gain channel to cover the entire dynamic range
  Both channels each cover 66 dB. Combined 84 dB capture in a single exposure.
Backside thinning flow had some issues:
  Imagers processed on SOI substrate showed a lot of hot cluster defects.
  Photoemission has been observed on these clusters
  Caused by impurities in the silicon that can not be gettered vertically because BOX is barrier
  Instead these impurities diffuse and are collected at n+ areas.
  If these n+ areas are at high potential, radiative recombination is observed, probably due to avalanche breakdown
  Issue is now fixed, fix demonstrated on an image sensor with 10 µm pixels and a new SOI processing run has just started on the BITFPA imager

## Slide 34: Acknowledgements
Ingrid De Wolf of IMEC for assistance with EMMI measurements
ESA for the support of this detector development in the frame of the ESA contract 4000100375/10/NL/RA “Back-illuminated Thinned CMOS Imager Focal Plane”

## Slide 35: Thank you
Guy Meynants
Founder & CTO
CMOSIS nv
Coveliersstraat 15
B-2600 Antwerp, Belgium
+32 3 260 17 32
guy@cmosis.com