## Slide 1
Hybrid Quantum Systems Composed of Superconducting Qubits, Nanomechanics, and Transmission Line Metamaterials
Matt LaHaye – Syracuse University
Photonics for Quantum WorkshopRIT 24 January 2019
CPB/NR/LC
Absorption
Spectrum
Image: LC Circuit-CPB-NR Spectroscopy
CPB-NR-LC Absorption Spectrum
Number-state-resolved Stark shift of transmon due to CPW Cavity Dispersive Interaction
Rabi Oscillations of transmon while coupled to NR and CPW Cavity
Plus some new ideas these systems have inspired related to quantum networking

## Slide 2: Outline
Recent Motivating Work
- Transmon-Coupled Nanoresonators
(LaHaye Group)
New Ideas:
- Superconducting Metamaterial Transmission Lines (Plourde Group)
- ~Recently published papers by theory collaborators using arrays/networks of transmon-coupled NRs for quantum simulation
- Metamaterials coupled to NR and superconducting qubits… potential applications for QIP (e.g. memory, transduction…)
Image from Plourde Group
LaHaye Group
From Tacchino et al. PRB 97, 214302 (2018)

## Slide 3
Development of Qubit-Coupled Mechanical Systems in the LaHaye Group at Syracuse
Suspended Mechanical Elements
DC-Biased Superconducting Microwave Cavities
Josephson-Junction based qubits
Fabrication at CNF & in Plourde Lab (SU)
Impetus: Develop qubit-coupled nano/micro/larger (!) mechanical systems as an architecture for exploring/utilizing quantum properties of motion at macroscale
Systems are analogous to circuit/cavity quantum electrodynamics (c/CQED) systems
Integrate
Integrate
Impetus: Develop the system as a resource for quantum information & quantum thermodynamics
Images from LaHaye Group (Fab by Hao and Rouxinol)

## Slide 4: cQED/CQED: A Resource for Mechanics
Asymmetric transmon (Plourde group & IBM) From M.Hutchings et al. Phy. Rev. Appl. 8, 044033 (2017)
Measurement of Microwave cavity number statistics via transmon (Schoelkopf Group) From D. Schuster et al. Nature 445, 515 (2007)
Fluxonium Qubit (Devoret Group)
From I. Pop et al. Nature 508, 370 (2014)
JJ-based qubits + cQED Technology offer the following
Strong non-linearities
Exquisite control
High quality coherence
By analogy, this technology can be utilized for engineering/measuring quantum mechanical states of motion & QIP with electromechanical elements
Characteristics used for explorations of quantum behavior in EM oscillators and QIP

## Slide 5
Abridged History of Quantum Electromechanics with Superconducting Qubits and Mechanical Modes
Short List of Qubit-Mechanics References
- A. Armour, M. Blencowe, & K.C. Schwab, PRL (2002)
- M.D. LaHaye et al., Nature (2009)
- A. O’Connell et al., Nature (2010)
- J. M. Pirkalainen et al., Nature (2013)
- Y. Chu, et al., Science (2017), Nature (2018)
- F. Rouxinol et al., Nanotechnology (2016)
Increasingly sophisticated
Experiments
Initial idea published on qubit-nanoresonator
First experimental demonstration
Using better circuitry/qubits
from cQED!
(Schoelkopf group) Mechanical quantum state control
LaHaye
Group
LaHaye et al. 2009 (Roukes Group)
O’Connell et al. 2010
(Cleland Group)
Pirkalainen et al. 2013
(Sillanpaa Group)

## Slide 6
Quantum Electromechanical Schematic – Transmon qubit, NR, CPW Cavity
F. Rouxinol, Y. Hao, F. Brito, A. Caldeira, E.K. Irish, and M. LaHaye. Nanotechnology 27, 364003(2016)
Transmon-NR coupling described by generalized, multi-level Jaynes-Cumming model:
Flexural,
UHF-range nanoresonator (NR)
Artificial Atom: the transmon
()
Transmon-NR coupling established by applying large (~ Volts) DC potential difference
Superconducting
CPW Cavity

## Slide 7
Design of Qubit-Mechanics Samples
SEM Image of Transmon Qubit and Circuitry
SEM Image of Nanoresonator (NR)
- Transmon embedded in ground plane of CPW cavity near a voltage anti-node of fundamental mode
- Devices engineered at CNF and SU (Plourde Lab), using optical/e-beam lithography and RIE etchs
Al Josephson junctions
Nb ground plane
Nb Flux
Bias loop
- Flux bias loop on chip for tuning transmon transition energy
Large Nb shunt capacitor
- Third in-plane flexural mode serves as NR, 5 GHz
- Suspended nanostructure fabricated from Al
- Separated from qubit by 35 nm
35 nm
F. Rouxinol, Y. Hao, F. Brito, A. Caldeira, E.K. Irish, and M. LaHaye. Nanotechnology 27, 364003(2016)
Silicon substrate
Can tune qubit thru this frequency
Low thermal occupation at mK temps
*Fab performed by F. Rouxinol, Y. Hao*

## Slide 8
Integrate transmon & NR into high-Q CPW cavity for dispersive measurement
CAD Drawing of Coplanar Waveguide Cavity
Coupling
Capacitor
Coupling Capacitors
CPW Cavity for Read-Out of Qubit-Mechanics
F. Rouxinol, Y. Hao, F. Brito, A. Caldeira, E.K. Irish, and M. LaHaye. Nanotechnology 27, 364003(2016)
Fundamental mode of cavity has
Embed qubit+NR in ground-plane near voltage anti-node of fundamental mode
Transmission of microwaves through CPW depends on state of the qubit
T-filter allows application of DC coupling voltage VNR without degrading Q-factor of the CPW (Q’s as high as 200,000 achieved)
See Hao, Rouxinol, LaHaye APL 105, 222603 (2014) for filter details

## Slide 9
Measurements of Resonant Interaction with NR (Perfromed by F. Rouxinol, Y. Hao)
Transmission Measurements of the Microwave Cavity with Qubit-NR Coupling Applied
Qubit Flux (
Qubit Flux (
Qubit Flux (
Cavity Probe Tone (
Cavity Probe Tone (
Cavity Probe Tone (
Amplitude (dBm)
Amplitude (dBm)
Amplitude (dBm)
- At low coupling (), cavity response varies with flux as expected due to interaction with qubit
- As is increased, a gap opens up in cavity response at value of flux where qubit and NR should be in resonance
Qubit energy = NR energy
Qubit energy = NR energy
Usual cavity response
- Resonant interaction between qubit and NR leads to hybridization* and shifts cavity response
(Sample on fridge at 30 mK)

## Slide 10
Measurement and Simulation of Resonant Interaction
Cavity Probe Tone (GHz)
Magnetic Flux Applied to Qubit ()
Data
Data
Data
Simulation
Simulation
Simulation
F. Rouxinol, Y. Hao, F. Brito, A. Caldeira, E.K. Irish, and M. LaHaye. Nanotechnology 27, 364003(2016)
Heating of NR is a design flaw that we know how to fix
Simulation: Lindblad master equation with coupled dynamics of CPW, qubit, & NR; relaxation & temperature terms for all three - Performed by collaborators: F. Brito (Sao Carlos), A. Caldeira (Campinas), E. Irish (Southampton)
only free parameter in the simulation – all others determined through other measurements
For all values of nano-resonator at low thermal occupation
(ie n<1)

## Slide 11
Measurement and Simulation of Resonant Interaction
Simulation: Lindblad master equation with coupled dynamics of CPW, qubit, & NR; relaxation & temperature terms for all three (Performed by collaborators: F. Brito (Sao Carlos), A. Caldeira (Campinas), E. Irish (Southampton)
Cavity Probe Tone (GHz)
Magnetic Flux Applied to Qubit ()
Data
Data
Data
Simulation
Simulation
Simulation
F. Rouxinol, Y. Hao, F. Brito, A. Caldeira, E.K. Irish, and M. LaHaye. Nanotechnology 27, 364003(2016)
only free parameter in the simulation – all others determined through other measurements
Did not observe quantum Rabi swapping or other coupled dynamics due to two design flaws: heating of NR due to parasitic substrate current and and low NR quality factor (clamping loss)

## Slide 12
Qubit as a Spectrometer* of NR Noise
Measurement of Qubit Linewidth Vs. Transition Energy
F. Rouxinol, Y. Hao, F. Brito, A. Caldeira, E.K. Irish, and M. LaHaye. Nanotechnology 27, 364003(2016)
NR quality factor was very low
Weak-coupling limit
In weak-coupling limit, NR acts like a dissipative bath*, leading to an increase in qubit linewidth as qubit is tuned through resonance with NR
*See Schoelkopf et al. arXiv:cond-mat/0210247 (2003)
Future Experiments to probe both +/- frequency noise terms also motivates using NR as an engineered reservoir quantum thermodynamics
NR Spectral Densities
NR Emission
NR Absorption

## Slide 13
New Mechanical Plate/Membrane Elements
Engineer strong coupling to transmons
Higher Q mechanical modes
Unfortunately, ran out of funding at this point…
Have higher Q: Q~1000 at 77K
Have not tested properties at milli-Kelvin temperatures
Lowest Mode Frequency ~ 80 MHz
Fabrication by Y. Hao

## Slide 14: Outline
Recent Motivating Work
- Transmon-Coupled Nanoresonators
(LaHaye Group)
New Ideas:
- Superconducting Metamaterial Transmission Lines (Plourde Group)
- ~Recently published papers by theory collaborators using transmon-coupled NRs for quantum simulation
- Metamaterials coupled to NR and superconducting qubits… potential applications for QIP (e.g. memory, transduction…)
Image from
Plourde Group
LaHaye Group
From Tacchino et al. PRB 97, 214302 (2018)

## Slide 15: Superconducting Metamaterial Transmission Lines - Motivation
Coupling a left-handed transmission line (LHTL) with a right-handed one (RHTL), results in dispersion relation that yields a dense set of modes that can couple strongly to a qubit (multi-mode strong coupling regime).
Location of inductors and capacitors swapped in LHTL
Spatial overlap of modes in RHTL enables modes to strongly coupled to a nearby qubit
Potential for multipartite entanglement generation, quantum simulation (e.g. spin boson model)

## Slide 16: Superconducting Metamaterial Transmission Lines – Periodic Array of Reactances
- To implement, need to fabricate a periodic array of lumped-element reactances
- Of course, real components have parasitic reactances
‘Falling’ Dispersion Relation
Density of modes diverges at zone edge
Parasites
Gap Opens in Dispersion Relation
See H. Wang et al. arXiv:1812.02579v1 for full expression
*Circuit schematics, figure from Plourde Group – H. Wang et al. arXiv:1812.02579v1 *
Infrared
Cut-off

## Slide 17: Superconducting Metamaterial Transmission Lines – Periodic Array of Reactances
- To implement, need to fabricate a periodic array of lumped-element reactances
- Of course, real components have parasitic reactances
‘Falling’ Dispersion Relation
Density of modes diverges at zone edge
Parasites
Still have infrared cut-off and divergence of density of modes
*Circuit schematics, figure from Plourde Group – H. Wang et al. arXiv:1812.02579v1 *
Gap Opens in Dispersion Relation
See H. Wang et al. arXiv:1812.02579v1 for full expression
in GHz range

## Slide 18
Superconducting Metamaterial Transmission Line Cavity – Resonant Modes
Adding a coupling capacitor to each end of the metamaterial results in a set of standing wave resonances
Coupling capacitor
Calculation of lower band resonance for cells using analytical expression for full dispersion relation
Usual Standing Wave Relation
Where labels mode number and is the number of cells
Notice that mode spacing decreases as increases as one would expect from dispersion relation
*Circuit schematics, figure from Plourde Group – H. Wang et al. arXiv:1812.02579v1 *

## Slide 19
Superconducting Metamaterial Transmission Line Cavity – Implementation (Plourde Group)
*Haozhi Wang et al. arXiv:1812.02579v1 *
Slide courtesy of
B. Plourde

## Slide 20
Superconducting Metamaterial Transmission Line Cavity – Transmission Characteristics (Plourde Group)
*Figures from Plourde Group – H. Wang et al. arXiv:1812.02579v1*
- Transmission () measurements reveal dense spectrum of modes with IR cut-off around 4 GHz
- Resonance frequencies follow expected dependence on from dispersion relation
Minimum mode spacing ~147 MHz

## Slide 21
Superconducting Metamaterial Transmission Line Cavity – Transmission Characteristics (Plourde Group)
*Figures from Plourde Group – H. Wang et al. arXiv:1812.02579v1*
- Transmission () measurements reveal dense spectrum of modes with IR cut-off around 4 GHz
- Resonance frequencies follow expected dependence on from dispersion relation
Minimum mode spacing ~147 MHz
Using Laser scanning microscopy (LSM) demonstrate spatial profile agrees with simulation & theory
LSM Imaging: Ustinov (Karlsruhe), Zhuravel (Verkin)

## Slide 22
Superconducting Hybrid Transmission Line Cavity – Integration with Transmon (Plourde Group)
*Figures from Plourde Group – Indrajeet *
Capacitively couple transmon to resonant modes of hybrid (LHTL-RHTL) transmission line
Use transmission measurements to probe the resonant interaction between each of the modes and the transmon as tune magnetic flux
JC Model
For Each Mode
Microwave tone routed to metamaterial
LHTL
RHTL
transmon

## Slide 23: Outline
Recent Motivating Work
- Transmon-Coupled Nanoresonators
(LaHaye Group)
New Ideas:
- Superconducting Metamaterial Transmission Lines (Plourde Group)
- ~Recently published papers by theory collaborators using transmon-coupled NRs for quantum simulation
- Metamaterials coupled to NR and superconducting qubits… potential applications for QIP (e.g. memory, transduction…)
Image from
Plourde Group
LaHaye Group
From Tacchino et al. PRB 97, 214302 (2018)

## Slide 24
New Idea: Integrate Metamaterial-Nanoresonator-Superconducting Qubit for Quantum Networking Apps.
LHTL
RHTL
transmon
Plourde Group
Integrate high-Q mechanics with transmon for implementing transmon-mediated quantum registry
LaHaye Group
Integration of these systems could yield multi-functional quantum network element
Integrate high-Q mechanics with LHTL/RHTL for enhanced parametric quantum transducer for data egress to photonic circuitry for distribution to larger network
High-Q, MHz-range mode
High-Q, GHz-range mode

## Slide 25: Application to Optical/Microwave Transduction
- One of the most promising approaches to optical/microwave transduction is based on opto-electro-mechanical devices
OPTOMECHANICAL CRYSTAL AND PIEZO IDT
Groblacher (Delft)
- Mechanism: parametric modulation of microwave and optical cavity by mechanical motion leads to up/down conversion of photons via
Superconducting LC Circuit and Optical Cavity
Regal,Lehenert (JILA)
- One main drawback: weak electromechanical coupling
Weak electromechanical anti-stokes process

## Slide 26: Metamaterial-Enhanced Optical/Microwave Transducer
- Could be difficult to increase , however, could use two closely-spaced modes of SMTL to resonantly enhance anti-stokes scattering
Resonantly Enhanced Anti-Stokes Scattering of Photons Using SMTL
Stokes still
Suppressed
- Tune the SMTL spectrum so that the difference in frequency between two adjacent modes is resonant with mechanical mode frequency
- Could this “boost” be enhanced further using more than two modes? Theory needs to be worked out.
Integrate Mechanical Element into SMTL
Typical Anti-Stokes Scattering of Photons
Stokes
Suppressed
Anti-Stokes
Anti-Stokes
enhanced
“Dual Mode” Transduction Theory Paper: Kippenberg, PRL 2010

## Slide 27: Metamaterial-Enhanced Optical/Microwave Transducer
Typical Anti-Stokes Scattering of Photons
Stokes
Suppressed
Integrate Optomechanical crystal with SMTL
Possibly use 3D integration techniques to engineer tight SMTL—NR-OMC coupling
Discussions with Plourde (SU), Papa Rao (SUNY Poly), Bhattacharya (RIT), Anlage (UMDCP), Hamilton & Adams (Auburn), Rouxinol (UNICAMP), Brito (Sao Carlos)
Anti-Stokes
- Tune the SMTL spectrum so that the difference in frequency between two adjacent modes is resonant with mechanical mode frequency
- Could this “boost” be enhanced further using more than two modes? Theory needs to be worked out.
Resonantly Enhanced Anti-Stokes Scattering of Photons Using SMTL
Stokes still
Suppressed
Anti-Stokes
enhanced
“Dual Mode” Transduction Theory Paper: Kippenberg, PRL 2010

## Slide 28: Quantum Electromechanical Memory/Registry
- Another promising possibility involves integration of SMTL, Transmon, & NR for implementation of quantum registry
Transmon
NR
LHTL
RHTL
- Utilize dispersive quantum switch operation between NR , and SMTL modes () mediated by qubit (transmon, )
Quantum
Switch
See: M. Mariantoni et al. Phys. Rev. B. 2008
- Mechanical Q’s in excess of a million demonstrated using phonon bandgap engineering (Painter, arXiv:1808.04874)

## Slide 29: Quantum Electromechanical Simulators
- Potential directions could be opened up with intensive investment of resources
J. Lozada-Vera, O. Neto, J. Moqadam, MD LaHaye & M.C. Oliveira. EPJ Quantum Tech. 3:9 (2016)
ARRAYS OF QUANTUM NANORESONATOR FOR QUANTUM SIMULATION/SENSING
Possibility of dense NR-Qubit arrays/networks for analog & digital quantum simulators
F. Tacchino, A. Chiesa, M.D. LaHaye, S. Carretta, & D. Gerace. PRB 97, 214302 (2018)

## Slide 30
Points to take home
Hybrid systems with superconducting metamaterials, NRs, and transmons could be versatile tools for Quantum Networking:
At SYR: Francisco Rouxinol (UNICAMP) & Yu Hao (SiTimes)
Theory Support: Fred Brito (Sao Carlos), Amir Caldeira (UNICAMP)
and Elinor Irish (Southampton)
Transmon/NR Experiments
Funding was provided by NSF-DMR Career Award #1056423/NSF-DMR Materials World Network Award #1312421
Optomechanical quantum transduction
Quantum electromechanical memory
Generation of complex entangled states
Quantum Simulation
Plourde Group Metamaterial Experiments:
B.L.T. Plourde, H.Wang, Indrajeet, M. Hutchins
Metamaterial Collaborators:
F. Wilhelm (Saarbrucken), A.V. Ustinov (Karlsruhe), F. Rouxinol, Y. Hao, B. Taketani (Saarbrucken), A.P. Zhuravel (Verkin)