## Slide 1: Germanium Charge-Coupled Devices for SWIR and X-Ray Imaging
C. Leitz, S. Rabe, I. Prigozhin, M. Zhu, B. Burke, K. Ryu, M. Cooper, R. Reich, K. Johnson, W. Hu, B. Felton, M. Cook, C. Stull, V. Suntharalingam
September 27, 2017
This material is based upon work supported under Air Force Contract No. FA8721-05-C-0002 and/or FA8702-15-D-0001. Any opinions, findings, conclusions or recommendations expressed in this material are those of the author(s) and do not necessarily reflect the views of the U.S. Air Force.
© 2017 Massachusetts Institute of Technology.
Delivered to the U.S. Government with Unlimited Rights, as defined in DFARS Part 252.227-7013 or 7014 (Feb 2014). Notwithstanding any copyright notice, U.S. Government rights in this work are defined by DFARS 252.227-7013 or DFARS 252.227-7014 as detailed above. Use of this work other than as specifically authorized by the U.S. Government may violate any copyrights that exist in this work.
DISTRIBUTION A. Approved for public release; distribution unlimited.

## Slide 2: MIT-LL Silicon Charge-Coupled Devices (CCDs)
Can we realize these advantages in other bands?
Exquisite sensitivity and dynamic range from soft X-ray to near infrared
Noiseless, efficient charge transfer enables time delay integration (TDI) operation, pixel binning
High spatial uniformity enables large-format imagers
PS1-2 (2007, 2015)
SST (2011, 2015)
TESS (2015)

## Slide 3: Motivation
SWIR & X-Ray Band Sensitivity [1-3]
[1] T. Martin & P. Dixon, Laser Focus World (11/2004); [2] MIT-LL measured; [3] average from Nakano et al., J. Non-Cryst. Sol. 358 (2012) 2249 & N. Posthuma et al., Proc. 3rd World Conf. Photo. Ener. Conv. (2003), scaled to 45 µm.
Disruptive Potential for Imaging in These Bands
Wafer Size Comparison
Sensor Size Comparison
200 mm
Germanium
InGaAs (SWIR)
CZT (X-ray)
InGaAs (1.3 Mpix)
5 cm
Germanium
(> 20 Mpix expected)
NuSTAR
(1 kpix)
High-quality gate dielectrics enable CCDs
No bump-bonding required
Compatible with Si CCD tool set

## Slide 4: Path to a Germanium CCD
Discrete devices provide insights into CCD performance
CCD Viewed Along Charge-Transfer Direction
Germanium substrate
Back surface electrode
Gate dielectric
Buried channel
Vlow
Vhigh
Vlow
Vlow
Vlow
Vhigh
VOG
Output
1
3
100 nm
Germanium
GeO2
Metal
Al2O3
2
C. Leitz et al., “Germanium CCDs for large-format SWIR and X-ray imaging,” Journal of Instrumentation 12 (2017).

## Slide 5: Estimating Dark Current in a Germanium CCD
Many key variables that govern device performance are nearly equivalent to silicon
Conservative dark current target of < 10 pA/cm2 at 150K
(40 e-/pixel/s for an 8-µm pixel)
Used measurements on building blocks to estimate dark current noise
Ge CCDs require cooling to achieve low dark current because of high intrinsic carrier conc.
Germanium
InGaAs
Silicon

## Slide 6: First-Generation Germanium Imagers
Reticle Layout
  1k × 2k × 8.1 µm frame transfer CCD
  128 × 128 x 8 µm OTCCD
  32 × 32 × 8.1 µm full-frame CCD
  Shift registers
  Shift registers
Single pixel
Metal Gate Detail
Processed 200-mm Wafer

## Slide 7: Germanium CCD Fabrication Challenges
Silicon CCD
Germanium CCD
Poly 1
Poly 2
Poly 3
Gap Between Phases
Silicon Dioxide
Gap Between Phases
Metal Gate Electrode
Gate Dielectric
Fabrication Challenge | Mitigation Plan | Other Alternatives
Cannot use overlapping poly-silicon process to define phases | Single-level CCD | Low-temperature fabrication processes
Charge transfer inefficiency due to large gap between phases | 248-nm lithography to define sub-300 nm gap | 193-nm or e-beam lithography
Low sensitivity in front illumination due to metal shading | Back illumination | Engineered substrate for rapid prototyping
Column isolation | Dopant-based isolation | Develop LOCOS process

## Slide 8: Diagnosis of First Ge CCDs
Unable to demonstrate charge transfer on devices from first wafer
Channel Stop
32-stage shift register
First CCDs saturated for all test conditions despite positive results from parametric tests (low diode leakage, no gate shorts)
Diagnosed problem as insufficient isolation from device periphery due to poorly functioning channel stop

## Slide 9: Diagnosis of First Ge CCDs
Results indicate poor isolation from periphery, indicating channel stop barrier height insufficient
Input Diode
Reset Drain
IG1
Only IG1 Biased
S1
S2
S3
Input Diode
Reset Drain
OG
IG2
IG1
RG
All Gates Biased
Contact

## Slide 10: Contributors to Low Channel Stop Barrier Height
Chart: Bias (V)
Chart: Depth (nm)
1. Lower-than-expected doping in channel stop
2. Rectifying contacts to channel stop region
  Measured dose = 1.5e12 cm-2
  Active dose = 1e11 cm-2
  Contact resistance ~ 104 Ω-µm2
  Contact resistance ~ 105 Ω-µm2
Addressed poor peripheral isolation by adjusting channel stop implant conditions
1018
1015
1017
1016
15
-15
0
10
5
-5
-10
Current (µA)
Total (SIMS)
Phosphorus Concentration (cm-3)
Electrically Active (SRP)

## Slide 11: Demonstration of Linear Germanium CCDs
Estimates of CCD performance from 32-pixel linear CCD
75,000 h+ well capacity (8.1 × 8.1 µm pixel)
0.6 nA/pixel dark current (-60°C)
CTE > 98.5% initially, drops to 85% over span of minutes
Improved isolation yields working 1-D Ge CCDs at -60°C
Input
Output
32 pixels
Chart: Input Bias (V)
| 4.5 | 4.3 | 4.0999999999999996 | 3.9 | 3.7 | 3.5 | 3.3 | 3.1 | 2.9 | 2.7 | 2.5
 | 0.6459 | 0.64911 | 0.65828 | 0.70704 | 0.8186 | 1.079 | 1.2409 | 1.2474 | 1.2529 | 1.2514 | 1.251
Well capacity
Dark Current

## Slide 12: Demonstration of 32 × 32 × 8.1 µm Array
Optical Micrograph of 32 × 32 Array
100 µm
Dark Response
Red LED Illumination
Subtracted Image
Scale: 4000-8000DN
Scale: -500-2000DN
Scale: 4000-8000DN
Further improvements to isolation led to operable pixel arrays at -60°C

## Slide 13: Next Steps
Device Testing
Test packaged shift registers and arrays in cryostat
Measure read noise, dark current
CTE Improvement
Characterize effect of field plate on shift registers
Fabricate devices with new metal mask (gaps shrunk from 230 nm  180 nm)
30 µm

## Slide 14: Conclusions
Germanium CCDs offer numerous advantages for X-ray and SWIR imaging
  Wide response
  Able to fabricate large-format CCDs on this material
Our work to date has validated the potential of germanium as a low-noise CCD material
Our first 32 × 32 CCDs are operational, and we are focused on improving CTE and scaling to larger arrays