## Slide 1
Performance of Science Grade HgCdTe H4RG-15 Image Sensors
Majid Zandian1, Mark Farris1, William McLevige1, Dennis Edwall1, Erdem Arkun1, Eric Holland1, James E Gunn2, Stephen Smee4, Donald N. B. Hall3, Klaus W. Hodapp3, Atsushi Shimon5, Naoyuki Tamura5, René Doyon6, Derrick Salmon7, Doug Simons7, Derek Ives8, Michael Carmody1, John Auyeung1, and James W. Beletic1
1Teledyne Imaging Sensors, 5212 Verdugo Way, Camarillo, CA 93012, USA
2Princeton University, 23 Payton Hall, Princeton, NJ 08544, USA
3University of Hawaii, Institute for Astronomy, 640 North A’ohoku Place, Hilo, HI 96720, USA
4John Hopkins University, 3400 N. Charles Street, Baltimore, MD 21218, USA
5Kavli Institute for the Physics and Mathematics of the Universe, 5-1-5 Kashiwanoha, Kashiwa, 277-8583, Japan
6University of Montreal, 2900 Edouard Montpetit Blvd, Montreal, QC H3T 1J4, Canada
7The Canada–France–Hawaii Telescope, 65-1238 Mamalahoa Hwy, Waimea, HI 96743, USA
8European Southern Observatory, Karl-Schwarzschild-Strasse 2, D-85748 Garching bei Munchen, Germany
2017 Scientific Detector Workshop
Space Telescope Science Institute, Baltimore, USA
25 - 29 September 2017
Supported by National Science Foundation Grant No. AST-0804651 through the University of Hawaii to Teledyne Imaging Sensors as well as contracts from University of Tokyo, Princeton University, University of Montreal, CFHT, and European Southern Observatory

## Slide 2: Outline
MBE HgCdTe Material for Large Format Arrays
H4RG-15 ROIC
H4RG-15 NIR and SWIR SCA Results
  Dark Current
  Quantum Efficiency
  Spectral Response
  CDS Noise
  Well Capacity
  Cross Talk
  SCA Flatness
Summary
4Kx4K H4RG-15

## Slide 3: MBE produces the highest performance HgCdTe
Molecular Beam Epitaxy (MBE)
  Enables very accurate deposition  “bandgap engineering”
  Teledyne has 4 MBE machines for detector growth
RIBER 5-inch MBE System
More than 10,000 HgCdTe wafers grown to date
Image of 7×7.5 cm HgCdTe layer grown in MBE-5
The black featureless surface is an excellent sign of HgCdTe quality.
3
Key Growth Parameters | Unit | 
Etch Pit Density | cm-2 | < 1E5
Carrier Concentration | cm-3 | 1.E+15
Micro Defect Density | cm-2 | < 1E4

## Slide 4: H4RG-15 ROIC Features
H1RG
H2RG
H4RG-15
H4RG-10
Preserved established features and performance of the H1RG and the H2RG
Add functionality and improved performance
All pads located on one side (top)
146 doubled I/O pads (probing and bonding)
Three-side close buttable
15 µm pixels
4k x 4k array.
Total dimensions:
63.36 x 66.17 mm²

## Slide 5: Outline
MBE HgCdTe Material for Large Format Arrays
H4RG-15 ROIC
H4RG-15 NIR and SWIR SCA Results
  Dark Current
  Quantum Efficiency
  Spectral Response
  CDS Noise
  Well Capacity
  Cross Talk
  SCA Flatness
Summary
4Kx4K H4RG-15

## Slide 6: Dark Current for NIR lc = 1.79 mm at 110K
I dark Map
I dark Histogram
T=110K SCA S/N 18315
Median Idark = 0.005 e-/sec/pixel
Idark Operability > 99 %

## Slide 7: Dark Current for SWIR lc = 2.45 mm at 80K
I dark Map
I dark Histogram
T=80K SCA S/N 18860
Median Idark = 0.007 e-/sec/pixel
Idark Operability > 99.8 %

## Slide 8: Dark Current vs Temperature
Chart: Temperature (K)
| 110 | 120 | 130
S/N 18315 (NIR 1.79 micron) | 0.006 | 0.019 | 0.023
S/N 18321 (NIR 1.78 micron) | 0.008 | 0.009 | 0.047
S/N 18661 (NIR 1.72micron) | 0.012 | 0.01 | 0.0066
S/N 18660 (NIR 1.73micron) | 0.016
S/N 18574 (SWIR 2.50 micron) | 0.016
S/N 18575 (SWIR 2.45 micron) | 0.0055
S/N 18564 (SWIR 2.55 micron) | 0.007
S/N 18586 (SWIR 2.55 micron) | 0.015
S/N 18788 (NIR 1.72 micron) | 0.008
S/N 18686 (SWIR 1.73 micron) | 0.026
S/N 18785 (NIR 1.72 micron) | 0.005
S/N 18859 (SWIR 2.43 micron) | 0.008
SWIR 2.5 mm
NIR 1.7 mm

## Slide 9: QE at 1230 nm for NIR lc = 1.79 mm at 120K
QE Map
QE Histogram
T=120K at 1230 nm SCA S/N 18315
Median QE > 80%
QE Operability > 99.4 %

## Slide 10: Spectral Response for NIR lc = 1.7 mm at 120K

## Slide 11: QE at 1230 nm for SWIR lc = 2.45 mm at 80K
QE Map
QE Histogram
T=80K at 1230 nm SCA S/N 18859
Median QE > 92%
QE Operability > 99.5 %

## Slide 12: Spectral Response for SWIR lc = 2.50 mm at 80K
Chart: Wavelength (nm)
SCA 18575 | 76 | 84.6 | 88.1 | 93.1 | 85.2
SCA 18860 | 93 | 96 | 98 | 99 | 79
SCA 18859 | 89 | 90 | 91 | 93 | 83
SCA 18574 | 74 | 87.4 | 99.1 | 99 | 94
Specification | 60 | 60 | 60 | 80 | 80 | 80 | 80
SCA 18574 | 74 | 87.4 | 99.1 | 99 | 94

## Slide 13: CDS Noise for NIR lc = 1.72 mm at 120K
CDS Noise Map
CDS Noise Histogram
T=120K SCA S/N 18788
Median CDS Noise = 19.4 e-
CDS Noise Operability > 99.7 %

## Slide 14: CDS Noise for SWIR lc = 2.45 mm at 80K
CDS Noise Map
CDS Noise Histogram
T=80K SCA S/N 18860
Median CDS Noise = 12 e-
CDS Noise Operability > 99.7 %
Chart: SCA index
NIR 1.7 um SCAs | 18.1 | 20.8 | 19.1 | 20 | 19 | 20
SWIR 2.5 um SCAs | 13.2 | 13.5 | 17.4 | 16 | 12 | 12
Standard Specification | 30 | 30 | 30 | 30 | 30 | 30
ESO-MOONS Specification | 15 | 15 | 15 | 15 | 15 | 15
Goal | 15 | 15 | 15 | 15 | 15 | 15

## Slide 15: Well Capacity for NIR and SWIR
T=80K SCA S/N 18575
Full Well >140 Ke @-250 mV
SWIR lc = 2.45 mm at 80K
T=120K SCA S/N 18315
Full Well >79 Ke @ -350 mV
NIR lc = 1.79 mm at 120K

## Slide 16
0.00%
0.9%
0.00%
1.30%
100%
1.30%
0.00%
1.00%
0.00%
Results consistent with detector model calculations
Total crosstalk results shows no dependence on temperature
Total Cross Talk for NIR and SWIR
189 events with charge in the 4,000 – 12,000 e- range.
We find a nearest neighbor total cross talk below about 1.1% and indistinguishable from the noise in the corner neighbors confirming the theoretically expected cross talk.
T=120K SCA S/N 18315
Total Cross Talk < 1.1%

## Slide 17
Maximum variation (peak-to-valley) to best fit plane was measured
Note: The flatness of SCA was measured using white light interferometry and entire SCA surface was imaged and analyzed.
Flatness of H4RG-15 SCAs as Low or better than H2RG
Peak to Valley =5.9 mm
RMS =0.8 mm

## Slide 18: Performance Summary of Science Grade H4RG-15 SCAs

## Slide 19
Four SWIR H4RG-15 SCAs (64 Mega Pixel FPA)

## Slide 20: Summary
  Fabricating and Testing Science Grade H4RG-15 NIR and SWIR SCAs
    Dark Current < 0.01 e-/s/p
    Quantum Efficiency > 70 %
    CDS Noise < 20 e-
    Well Capacity > 70 Ke-
    Cross Talk < 1 %
    Operability > 95 %
    SCA Flatness < 20 mm
  Growing Low Defects Density MBE Layers on 7x7.5 cm2 CdZnTe Substrates
  H4RG-15 ROIC Fabrication at ON-Semiconductor. Preserved Established Features and Performance of H1RG and H2RG
  Using Invar Pedestal for H4RG-15 Package